## Slide 1
by
MD. FARHAN – 1710035
and
MD. SHAHED HOSSAIN SOHAN - 1710043
under the supervision of
DR. MD. ASHIQUR RAHMAN
Professor, Dept. of Mechanical Engineering Bangladesh University of Engineering & Technology
Analysis of Mechanical Properties of Crumpled Graphene: A Molecular Dynamics Approach

## Slide 2
BACKGROUND
(a)
(b)
Figure 01: Atomistic schematic of (a) Graphene[1] and
(b) Crumpled Graphene[2].
Graphene
Flexible, strong, high elastic modulus
Crumpled Graphene
Large specific surface areas, improved conductivity, higher specific capacitance.
ME 400

## Slide 3
MOTIVATION
Application of Crumpled Graphene
Energy Storage
Electronics & Sensors
Catalysis
Biomedical application
Source: Internet.

## Slide 4
Supercapacitors experience Thermal expansion or other kinds of deformations.
Deformation changes the promising characteristics
Figure 02: Fabrication process for the load-bearing supercapacitor fabrics.[3]
MOTIVATION

## Slide 5
Mechanical performance analysis of non-porous crumpled graphene under uniaxial tensile load for different degree of crumpling.
Performance analysis of porous crumpled graphene under uniaxial tensile load for different degree of crumpling.
Comparison of strain energy due to deformation both in porous and non porous cases.
Mechanical performance analysis under uniaxial compressive test.
ME 400
OBJECTIVES

## Slide 6
Molecular Dynamics
Platform: Large-scale Atomic/Molecular Massively Parallel Simulator (LAMMPS), OVITO
Potential: Adaptive Intermolecular Reactive Empirical Bond Order (AIREBO).
SIMULATION & METHODOLOGY

## Slide 7
Crumpling process
Potential: AIREBO
Size: 50Å x 50Å
Buehler et al.[2]
Initialization
Equilibration
Final run
Crumpling
r =
r = 26.5 Å
r = 19.3 Å
r = 7.6 Å
SIMULATION & METHODOLOGY

## Slide 8
Addition of Porosity
Percentage Porosity | Number of atoms
0% | 960
5% | 912
10% | 864
20% | 768
30% | 672
0% Porosity
10% Porosity
ME 400
-Perforated graphene
-Randomly added defects[2]
SIMULATION & METHODOLOGY

## Slide 9
Tensile Loading
Methods:
Rescaling method
Displacement control method
Parameters:
Strain rate: 0.001 ps-1 or 109 s­­-1
Timesteps: 0.0005ps
Relaxation: 1ps
Temperature: 300 K
Boundary Condition: p p s
Figure 03: Tensile load along y axis by displacement control method
SIMULATION & METHODOLOGY
z
y

## Slide 10
Tensile Loading
Displacement control method
SIMULATION & METHODOLOGY

## Slide 11
Compressive Loading and
unloading
Displacement control method
Parameters:
Strain rate: 0.02 ps-1
Timesteps: 0.0002ps
Relaxation: 30ps
Temperature: 300 K
Boundary Condition: s p p
Figure 04: Compressive load along y axis by displacement control method
y
z
x
SIMULATION & METHODOLOGY

## Slide 12
Compressive Loading
Displacement control method
SIMULATION & METHODOLOGY

## Slide 13
Fracture under Uniaxial Tensile Load on Non-porous CGs
Figure 05: Variation of stress as a function of strain at different levels of crumpling in graphene.
Results And Discussion

## Slide 14
Figure 06: Variation of stress as a function of strain for flat graphene at different levels of porosity.
Results And Discussion
Fracture under Uniaxial Tensile Load on Porous CGs

## Slide 15
Figure 07: Variation of stress with strain in case of a CG with 19.3 Å at different porosity level.
Results And Discussion
Fracture under Uniaxial Tensile Load on Porous CGs

## Slide 16
Figure 08: Variation of stress with strain in case of a CG with 14.7 Å at different porosity level.
Results And Discussion
Fracture under Uniaxial Tensile Load on Porous CGs

## Slide 17
Figure 09: Variation of stress with strain in case of a CG with 7.6 Å at different porosity level.
Porosity , Stress
Porosity ,Stress
Critical Radius
Results And Discussion
Fracture under Uniaxial Tensile Load on Porous CGs

## Slide 18
Crumpling Radius, Å | Fracture Toughness, GPa |  | 
 | Non porous Graphene | With 10% porosity | With 20% porosity
Infinite (Flat) | 120 | 50 | 30
24.3 | 13.7 | 8.8 | 7.2
19.3 | 10.5 | 3.5 | 7
14.7 | 18 | 16 | 3.5
12.3 | 29.5 | 23 | 14
7.6 | 49.5 | 26 | 18
ME 400
Results And Discussion

## Slide 19
Figure 10: Variation in Elastic Modulus with change in crumpling radius.
Stiffness does not vary with crumpling radius with more porosity.
Significant Carbon-Carbon bond has been lost.
Results And Discussion
Stiffness under Uniaxial Tensile Load

## Slide 20
Figure 11: Variation of elastic modulus with % of porosity in electrode at different degree of crumpling.
With larger crumpling radii, the effect of porosity on the elastic modulus is less important.
Results And Discussion
Stiffness under Uniaxial Tensile Load

## Slide 21
Figure 12: Variation of stress with strain for 7.6 Å CG for uniaxial tension added towards x, y and z directions.
Due to presence of symmetry loading in y and z direction shows better performance.
Results And Discussion
Tensile Load along x, y and z directions

## Slide 22
Results And Discussion
Tensile Load along x, y and z directions

## Slide 23
Figure 12 : Variation of strain energy in Flat graphene with applied strain at different degree of porosity.
Results And Discussion
Strain Energy under Uniaxial Tensile Load

## Slide 24
Figure 13: Variation of strain energy in crumpled graphene with applied strain at different degree of porosity with crumpling radius 12.3 Å.
Strain Energy under Uniaxial Tensile Load
Results And Discussion

## Slide 25
Compressive Load along x-axis
Figure 14: Variation of stress as a function of strain under uniaxial compressive load along x direction.
Results And Discussion

## Slide 26
Figure 15: Variation of stress with strain under uniaxial compressive loading along y direction.
Compressive Load along y-axis
Results And Discussion

## Slide 27
Validation
Figure 16: Variation of stress with applying strain along the armchair direction on a flat graphene.[4]

## Slide 28
Validation
References | Methods | Elastic Modulus, GPa
Arroyo and Belytschko[5] | Continuum models | 694
Kudin and Scuseria[6] | Ab initio and Quantum | 1021
Ni and Bu[7] | MD simulations | 1100
Tsai and Tu[8] | MD simulations | 912
Georgantzinos et al. [9] | Finite element method | 1367
Li and Chou[10] | Structural molecular mechanics | 1033
Lee et al.[11] | Experiment | 1033
Yupeng and Pan[12] | Experiment | 891
Present study | MD simulation | 835
Table 1: Young's modulus values as reported in articles.

## Slide 29
Conclusion
Crumpling initially decreases the fracture toughness, elastic modulus as well as the strain energy of crumpled graphene up to a crumpling radius of 19.3 Å, beyond which it becomes more stress-resistant with additional crumpling.
Porosity has an adverse effect on these mechanical parameters. Nevertheless, the negative impacts of porosity due to higher crumpling levels i.e., lower radius, can be partially mitigated within a specific range.
Shape of the crumpled graphene considered has great impact on its mechanical behavior.
CG deforms plastically under compressive loading and retains its deformed shape after unloading, depending on its morphology.

## Slide 30
Future Recommendation
Analysis with a larger graphene sheet.
The effect of incremental strain can be observed to increase the scope of the study.
The effect of compressive loading on porous CG can be an interesting field to explore.
Composite materials with improved mechanical properties by embedding metallic nanoparticles (such as Ni, Cu).

## Slide 31
Thank You

## Slide 32
Appendix
Equations

## Slide 33
Appendix
1. Roberts, M., et al., Continuum Plate Theory and Atomistic Modeling to Find the Flexural Rigidity of a Graphene Sheet Interacting with a Substrate. Journal of Nanotechnology, 2010. 2010.
Buehler, S., Packing efficiency and accessible surface area of crumpled graphene. Phys. Rev. B, 2011. 84.
Shen, C., et al., Wearable woven supercapacitor fabrics with high energy density and load-bearing capability. Scientific Reports, 2017. 7.
Dewapriya, N., A.S. Phani, and N. Rajapakse, Influence of temperature and free edges on the mechanical properties of graphene. Modelling and Simulation in Materials Science and Engineering, 2013. 21: p. 065017
Arroyo, M., Finite Crystal elasticiy of carbon nanotubes based on the exponential Cauchy-Born rule. Phys. Rev. B, 2004. 69.
Kudin, K., G. Scuseria, and B. Yakobson, C2F, BN, and C nanoshell elasticity from ab initio computations. Physical Review B, 2001. 64: p. 235406.
References

## Slide 34
Appendix
References
6. Ni, Z., et al., Anisotropic mechanical properties of graphene sheets from molecular dynamics. Physica B-condensed Matter - PHYSICA B, 2010. 405: p. 1301-1306.
Tsai, J.-L. and J.-F. Tu, Characterizing mechanical properties of graphite using molecular dynamics simulation. Materials & Design, 2010. 31: p. 194–199.
Georgantzinos, S.K., G. Giannopoulos, and N.K. Anifantis, Numerical investigation of elastic mechanical properties of graphene structures. Materials and Design, 2010. 31: p. 4646-4654.
Li, C. and T.-W. Chou, A structural mechanics approach for the analysis of carbon nanotubes. International Journal of Solids and Structures, 2003. 40: p. 2487-2499.
Lee, C., et al., Measurement of the Elastic Properties and Intrinsic Strength of Monolayer Graphene. Science (New York, N.Y.), 2008. 321: p. 385-8.
Zhang, Y. and C. Pan, Measurements of mechanical properties and number of layers of graphene from nano-indentation. Diamond and Related Materials, 2012. 24: p. 1–5.

## Slide 35
Figure: Crumpled Graphene.
Figure06: Different crumpling method.
Source: Wikipedia
Appendix

## Slide 36
Figure: Stress strain curve
[Dewapriya et al. 2008]
Source: Wikipedia
Appendix

## Slide 37
Source: Wikipedia
    Graphene synthesis
    Mechanical exfoliation
    Chemical vapor deposition
    Epitaxial growth
    Crumpled Graphene synthesis
Aerosol spray drying method
Hydrothermal method
Thermal reduction of graphene oxide method
Mechanical method
Appendix

## Slide 38
Figure: Nanoindentation of suspended graphene membrane.
[Lee et al. 2008]
Source: Wikipedia
Appendix

## Slide 39
Figure: Compression of polystyrene.
[Akbari et al. 2020]
Source: Wikipedia
Appendix

## Slide 40
Source: Wikipedia
Appendix